Supporting information

Synthesis and Combustion Performance Investigation of Fe2O3-containing Nanothermites via Ball Milling Method

Aifeng Jiang, Debin Xia, Mengru Li, Kaifeng Lin, Liangsheng Qiang, Jiahe Li, Ruiqing Fan,* and Yulin Yang*

MIIT Key Laboratory of Critical Materials Technology for New Energy Conversion and Storage, School of Chemistry and Chemical Engineering, Harbin Institute of Technology, Harbin 150001, P. R. China.

E-mail addresses: fanruiqing@hit.edu.cn (R.Q. Fan), ylyang@hit.edu.cn (Y.L. Yang).

Table of Contents

Section 1. SEM image and contact angle of Fe2O3 nanoparticles	S-3

Section 2. TGA fitting curves of nanothermites prepared by in-situ ball milling and ultrasonic blending method	S-4

Section 1. SEM image and contact angle of Fe2O3 nanoparticles.

Figure S1.  SEM image of Fe2O3 nanoparticles.

Figure S2.  Contact angle of Fe2O3 nanoparticles.

Section 2. TGA fitting curves of nanothermites prepared by in-situ ball milling and ultrasonic blending method.

Figure S3.  TGA fitting curves of nanothermites prepared by in-situ ball milling method, (a) nano-Al doped 1 wt% Fe2O3; (b) nano-Al doped 5 wt% Fe2O3; (c) nano-Al doped 9 wt% Fe2O3; (d) nano-Al doped 13 wt% Fe2O3; (e) nano-Al doped 17 wt% Fe2O3; (f) nano-Al doped 21 wt% Fe2O3.

Figure S4.  TGA fitting curves of nanothermites prepared by ultrasonic blending method, (a) nano-Al doped 1 wt% Fe2O3; (b) nano-Al doped 5 wt% Fe2O3; (c) nano-Al doped 9 wt% Fe2O3; (d) nano-Al doped 13 wt% Fe2O3; (e) nano-Al doped 17 wt% Fe2O3; (f) nano-Al doped 21 wt% Fe2O3.

Table S1.  TGA fitting curves constants of nanothermites prepared by in-situ ball milling method.

| fBx=B1*x3+B2*x2+B3*x+intercept |  |  |  |  |
| --- | --- | --- | --- | --- |
| Doped amount | B1 | B2 | B3 | Intercept |
| 1 wt% | 1.089*10-7 | -7.997*10-5 | 0.0179 | 99.118 |
| 5 wt% | 1.046*10-7 | -6.623*10-5 | 0.0141 | 99.287 |
| 9 wt% | 9.745*10-8 | -5.364*10-5 | 0.0101 | 99.530 |
| 13 wt% | 8.798*10-8 | -3.921*10-5 | 0.00478 | 99.761 |
| 17 wt% | 7.510*10-8 | -1.798*10-5 | -0.00143 | 100.038 |
| 21 wt% | 6.213*10-8 | -3.476*10-6 | -0.00526 | 100.365 |

Table S2.  TGA fitting curves constants of nanothermites prepared by ultrasonic blending method.

| fSx=S1*x3+S2*x2+S3*x+intercept |  |  |  |  |
| --- | --- | --- | --- | --- |
| Doped amount | S1 | S2 | S3 | Intercept |
| 1 wt% | 9.466*10-8 | -5.920*10-5 | 0.0157 | 98.704 |
| 5 wt% | 9.313*10-8 | -5.652*10-5 | 0.0165 | 98.603 |
| 9 wt% | 9.694*10-8 | -6.093*10-5 | 0.0160 | 98.709 |
| 13 wt% | 9.095*10-8 | -5.852*10-5 | 0.0163 | 98.746 |
| 17 wt% | 9.221*10-8 | -6.109*10-5 | 0.0181 | 98.658 |
| 21 wt% | 8.499*10-8 | -5.396*10-6 | 0.0152 | 98.879 |

Table S3.  Constants of TGA fitting curves derivatives of nanothermites prepared by in-situ ball milling method.

| fBx=B1'*x2+B2'*x+B3' |  |  |  |  |
| --- | --- | --- | --- | --- |
| Doped amount | B1' | B2' | B3' | Weight gain percentage per 100 ℃ |
| 1 wt% | 3.267*10-7 | -1.599*10-4 | 0.0179 | 11.8% |
| 5 wt% | 3.138*10-7 | -1.325*10-4 | 0.0141 | 12.9% |
| 9 wt% | 2.924*10-7 | -1.073*10-4 | 0.0101 | 13.0% |
| 13 wt% | 2.639*10-7 | -7.842*10-5 | 0.00478 | 12.9% |
| 17 wt% | 2.253*10-7 | -3.596*10-5 | -0.00143 | 13.1% |
| 21 wt% | 1.864*10-7 | -6.952*10-5 | -0.00526 | 12.4% |

Table S4.  Constants of TGA fitting curves derivatives of nanothermites prepared by ultrasonic blending method.

| fSx=S1'*x2+S2'*x+S3' |  |  |  |  |
| --- | --- | --- | --- | --- |
| Doped amount | S1' | S2' | S3' | Weight gain percentage per 100 ℃ |
| 1 wt% | 2.840*10-7 | -1.184*10-4 | 0.0157 | 12.0% |
| 5 wt% | 2.794*10-7 | -1.130*10-4 | 0.0165 | 12.2% |
| 9 wt% | 2.908*10-7 | -1.219*10-4 | 0.0160 | 12.2% |
| 13 wt% | 2.729*10-7 | -1.170*10-4 | 0.0163 | 11.4% |
| 17 wt% | 2.766*10-7 | -1.222*10-4 | 0.0181 | 11.4% |
| 21 wt% | 2.550*10-7 | -1.079*10-4 | 0.0152 | 10.8% |